Supporting Information

Selective Charge Extraction allows Fast Photomultiplication and Imaging in Rigid and Ultra-flexible SWIR Organic Photodiodes

Matilde Brunetta1,2, Zhuoran Qiao3, Davide Nodari3, Kosei Sasaki4, Francesco Furlan3, Martina Rimmele3, Hongki Kim3, Hongting Chen4, Yusaku Tagawa4, Adam Marsh5, Rushil Vasant6, Sang Do6, Xabier Rodríguez-Martínez7, Anirudh Sharma5, Christos L. Chochos8, Jaime Martin7, Martin Heeney3,5, Koen Vandewal9, Derya Baran5, Thuc-Quyen Nguyen6, Bob C. Schroeder2, Takao Someya4, Tomoyuki Yokota4,10, Nicola Gasparini3*

1Department of Materials, Molecular Science Research Hub, Imperial College, London W12 0BZ, United Kingdom

2Department of Chemistry, University College London, 20 Gordon Street, London WC1H 0AJ, United Kingdom

3Department of Chemistry and Centre for Processable Electronics, Imperial College London, London W120BZ, United Kingdom

4Department of Electrical Engineering and Information Systems, The University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8656, Japan

5King Abdullah University of Science and Technology (KAUST), Division of Physical Sciences & Engineering (PSE), Chemistry Program, Thuwal 23955, Saudi Arabia

6 Center for Polymers and Organic Solids (CPOS), Department of Chemistry and Biochemistry, University of California at Santa Barbara, Santa Barbara, CA, 93106 USA

7Universidade da Coruña, Campus Industrial de Ferrol, CITENI, Ferrol, 15403, Spain

8Institute of Chemical Biology, National Hellenic Research Foundation (NHRF), 48 Vassileos Constantinou Avenue, Athens, 11635 Greece

9Institute for Materials Research (IMO-IMOMEC), Hasselt University, Diepenbeek, Belgium and IMEC Division, IMOMEC, Diepenbeek, Belgium

10Institute of Engineering Innovation, Graduate School of Engineering, The University of Tokyo, 7-3-1 Bunkyo-ku, Tokyo, 113-8656, Japan

Keywords: ultralow band gap polymer, photomultiplication, organic photodetector, biomedical sensor, IR detection, pulse oximeter, flexible organic photodetector

Correspondence to n.gasparini@imperial.ac.uk

Supplementary Figures

TQ-3T was synthesised according to literature procedures[1]. All chemical and solvents were purchased from commercial suppliers and used without further purification. TQ-3T was synthesised in lower molecular weight (Supplementary Fig. S1) compared to previously reported in literature which benefits the processability of the blend in chloroform.

Figure S1: Size exclusion chromatogram of TQ-3T, obtained using trichlorobenzene at 150oC.

Figure S2: UPS and LE-IPES spectra of pristine TQ-3T showing (a) the secondary electron cut-off and (b) the valence region of UPS spectra. (c) LE-IPES spectra showing the onset corresponding to the electron affinity.

Figure S3: UPS and LE-IPES spectra of pristine Y6 showing (a) the secondary electron cut-off and (b) the valence region of UPS spectra. (c) LE-IPES spectra showing the onset corresponding to the electron affinity.

Figure S4: 2D GIWAXS images and in-plane and out-of-plane scattering profiles. (a) 2D GIWAXS image of doctor blade coated TQ-3T:Y6 1:1 (wt/wt). (b) In-plane and out-of-plane scattering profiles integrated from 2D GIWAXS patterns. (c) 2D GIWAXS images of spin coated TQ-3T:Y6 1:1 (wt/wt). (d) In-plane and out-of-plane scattering profiles integrated from 2D GIWAXS patterns.

Figure S5: Contact-mode AFM topography. AFM image (5 × 5 µm² scan area) of TQ-3T:Y6 1:1 (wt/wt) blend.

Figure S6: Current density-voltage (J-V) characteristics of TQ-3T:Y6. J-V characteristics from -10 V to 2 V of TQ-3T:Y6 (2:1, 1:1 and 1:2, wt/wt) OPDs under AM1.5G illumination and in dark conditions.

Figure S7: Bias-dependent spectral responsivity. Spectral responsivity of TQ-3T:Y6 (1:1, wt/wt) at -2 V (dashed line) and -10 V (solid line).

Figure S8: Optoelectronic properties of HTL-free conventional architecture OPD based on TQ-3T:Y6. (a) Energy band diagram of HTL-free conventional architecture TQ-3T:Y6 (1:1, wt/wt) OPD. (b)  J-V characteristics in both dark and light conditions of HTL-free conventional architecture TQ-3T:Y6 (1:1, wt/wt) OPD. (c) Bias-dependent external quantum efficiency (EQE) at -10 V showing PM effect.

Figure S9: Optoelectronic properties of HTL-free inverted architecture OPD based on TQ-3T:Y6. (a) Energy band diagram of HTL-free inverted architecture TQ-3T:Y6 (1:1, wt/wt) OPD. (b) J-V characteristics in both dark and light conditions of HTL-free inverted architecture TQ-3T:Y6 (1:1, wt/wt) OPD. (c) Bias-dependent external quantum efficiency (EQE) at -10 V.

Figure S10: ‘hole-only’ OPD based on TQ-3T:Y6 with both PEDOT:PSS and MoOx as transport layers. (a) Energy band diagram of ‘hole-only’ TQ-3T:Y6 (1:1, wt/wt) OPD with both PEDOT:PSS and MoOx as transport layers. (b) J-V characteristics in both dark and light conditions of ‘hole-only’ TQ-3T:Y6 (1:1, wt/wt) OPD. (c) Bias-dependent external quantum efficiency (EQE) at -10 V showing PM effect.

Figure S11: Optoelectronic properties of inverted architecture OPDs based on BHJs with TQ-3T as donor and PC71BM and IEICO-4F as acceptors. (a) Energy band diagram of inverted architecture OPDs based on TQ-3T and different acceptors with a different mobility (Supplementary Table S1) compared to Y6 (also shown). (b) J-V characteristics in both dark and light conditions of inverted architecture TQ-3T:IEICO-4F (1:1, wt/wt) OPD. (c) Bias-dependent external quantum efficiency (EQE) of inverted architecture TQ-3T:IEICO-4F (1:1, wt/wt) OPD. (d) J-V characteristics in both dark and light conditions of inverted architecture TQ-3T:PC71BM (1:1, wt/wt) OPD. (c) Bias-dependent external quantum efficiency (EQE) of inverted architecture TQ-3T:PC71BM (1:1, wt/wt) OPD.

Figure S12: Space-charge-limited-current (SCLC) curves of both hole and electron mobilities. (a) SCLC curve of hole-only mobility in TQ-3T. (b) SCLC curve of electron-only mobility in Y6. The fittings are taken for the same current-voltage region.

Figure S13: Current density-voltage characteristics of ultrathin flexible TQ-3T:Y6 PM-OPD. J-V characteristics in both dark and light conditions of inverted architecture TQ-3T:Y6 (1:1, wt/wt) OPD, before and after peeling off their temporary glass support.

Figure S14: Current density-voltage (J-V) characteristics of TQ-3T:Y6 fresh and aged 10 months. J-V characteristics from -10 V to 2 V of TQ-3T:Y6 (1:1, wt/wt) OPDs under AM1.5G illumination and in dark conditions.

Figure S15: Bias-dependent photoplethysmogram (PPG) waveforms at 780 nm, 940 nm and 1100 nm. (a) Bias-dependent PPG waveform of TQ-3T:Y6 (1:1, wt/wt) based flexible OPD upon 780 nm illumination. (b) Bias-dependent PPG waveform of TQ-3T:Y6 (1:1, wt/wt) based flexible OPD upon 940 nm illumination. (c) Bias-dependent PPG waveform of TQ-3T:Y6 (1:1, wt/wt) based flexible OPD upon 1100 nm illumination.

Supplementary Tables

| OPD | Jsc (mA cm-2) | Voc (V) | FF (%) | PCE (%) | Jd (A cm-2) @ -2V |
| --- | --- | --- | --- | --- | --- |
| TQ-3T:Y6 (1:1) | 3.05 | 0.16 | 29.7 | 0.14 | 2.7 × 10-4 |
| TQ-3T:Y6 (2:1) | 0.82 | 0.19 | 34.2 | 0.04 | 1.3 × 10-4 |
| TQ-3T:Y6 (1:2) | 3.13 | 0.14 | 27.4 | 0.12 | 1.2 × 10-3 |
| TQ-3T:IEICO-4F | 1.41 | 0.31 | 46.5 | 0.20 | 2.7 × 10-5 |
| TQ-3T:PC71BM | 2.35 | 0.34 | 43.6 | 0.35 | 1.1 × 10-5 |
| Flexible TQ-3T:Y6 (1:1) before peeling | 0.83 | 0.17 | 25.6 | 0.04 | 1.4 × 10-4 |
| Flexible TQ-3T:Y6 (1:1) after peeling | 0.49 | 0.16 | 21.5 | 0.01 | 1.9 × 10-4 |

Table S1: Photodiode parameters extracted from J-V curves of OPDs reported in this study. The values are representative of at least 10 devices.

| Acceptor | e- mobility (cm2/Vm) |
| --- | --- |
| IEICO-4F | 1.15 × 10−4 [2] |
| Y6 | 1.84 × 10-4 |
| PC71BM | ~10-3 [3] |

Table S2: Electron mobilities of acceptors used in this study.

| Device architecture | Spectral range (nm) | EQE (%) | Bias (V) | D* or D*sh (Jones) | Speed (τr/τf)(ms) | Refs |
| --- | --- | --- | --- | --- | --- | --- |
| Trap-assisted carrier injection |  |  |  |  |  |  |
| ITO/ZnO/P3HT:4Bx/MoOx/Ag | 300-800 | 64000 | 20 | 4.28×1012 | - | [4] |
| ITO/TAPC/AIE:C70/C70/MoOx/C70/BCP/Al | 300-700 | 25000 | 6 | 3.08×1012 | 1.69/10 | [5] |
| ITO/ZnO/PBDB-T:Y6/MoOx/Ag | 300-1000 | 8133 | 2 | 4.23×1012 | 0.02/0.59 | [6] |
| ITO/ZnO/PBDB-T:Y6/QDs/Ag | 300-900 | 6565 | 3 | 4.9×1012 | -/0.04 | [7] |
| ITO/TAPC/PbPc:C70/C70/MoOx:C70/BCP/Al | 300-1000 | 6000 | 8 | 1×1012 | 16.3/33.7 | [8] |
| ITO/PEDOT:PSS/Poly-TPD:P3HT:PCBM/ Al | 300-700 | 3600 | 20 | 1×1012 | - | [9] |
| ITO/ZnO/PM6:Y6/CsPbI3 QDs/Ag | 300-900 | 2000 | 3 | 1×1012 | 0.00035/- | [10] |
| ITO/ZnO/PCE-10:COTIC-4F:BFDO-4F/MoOx/Ag | 300-1200 | 5708 | 2.5 | 1.13×1012 | 2.37/0.58 | [11] |
| ITO/ZnxO:D149/PBDB-T:ITIC-Th/e-Zano/Ag | 400-900 | 3000 | 2 | 1.5×1012 | 0.03958/0.037614 | [12] |
| Blocking-induced band bending |  |  |  |  |  |  |
| ITO/ZnO/BHJ/BCP/Ag | 300-1200 | 113702 | -2 | 5.7×1013 | 0.25/1.17 | [13] |
| ITO/TAPC/PbPc/HAT-CN/BCP/Al | 300-1000 | 5675 | 6 | 5×1011 | - | [14] |
| Ag/IB/HBL/C60:D6/ETL/Ag | 300-1100 | 3000 | 9 | 1×1013 | - | [15] |
| ITO/HBL/HBL:C60/ZnPc:C60/ HATN-Cl6/Al | 400-900 | 1290 | -8 | 1.7×1012 | 0.022/ 0.027 | [16] |
| ITO/HBL/C70/TAPC:C70/BCP/Al | 300-800 | 122270 | -6 | 5.9×1012 | - | [17] |
| ITO/ZnO/BHJ/Bphen/Ag | 600-1400 | 660 | -8 | <109 | -/1 | [18] |
| ITO/ZnO/TQ-3T:Y6/MoOx/Ag | 350-1450 | 1129 | -10 | 1.5×1010 | 0.073/ 0.076 | This work |

Table S3: Summary of key performance parameters of PM-OPDs

SI References

[1]	P. Jacoutot, A. D. Scaccabarozzi, D. Nodari, J. Panidi, Z. Qiao, A. Schiza, A. D. Nega, A. Dimitrakopoulou-Strauss, V. G. Gregoriou, M. Heeney, C. L. Chochos, A. A. Bakulin, N. Gasparini, Sci. Adv. 2023, 9, DOI 10.1126/sciadv.adh2694.

[2]	Z. Wang, H. Jiang, X. Liu, J. Liang, L. Zhang, L. Qing, Q. Wang, W. Zhang, Y. Cao, J. Chen, J. Mater. Chem. A Mater. 2020, 8, 7765.

[3]	B. Ebenhoch, S. A. J. Thomson, K. Genevičius, G. Juška, I. D. W. Samuel, Org. Electron. 2015, 22, 62.

[4]	J. Kim, H. Kweon, M. Lee, M. Kang, S. Lee, S. An, W. Lee, S. Choi, H. Choi, Y. Seong, H. Ham, H. Cha, J. Lim, D. H. Kim, B. Kim, D. S. Chung, Advanced Materials 2023, 35, DOI 10.1002/adma.202302786.

[5]	D. Guo, Z. Xu, D. Yang, D. Ma, B. Tang, A. Vadim, Nanoscale 2020, 12, 2648.

[6]	Q. Liu, L. Li, J. Wu, Y. Wang, L. Yuan, Z. Jiang, J. Xiao, D. Gu, W. Li, H. Tai, Y. Jiang, Nat. Commun. 2023, 14, 6935.

[7]	S. G. Han, H. Lee, W. Choi, D. Lee, S. Kim, Y. Sung, S. Kim, K. Cho, Adv. Funct. Mater. 2021, 31, DOI 10.1002/adfm.202102087.

[8]	D. Guo, L. Yang, J. Li, G. He, J. Zheng, S. Tao, D. Yang, L. Wang, A. Vadim, D. Ma, Sci. China Mater. 2023, 66, 1172.

[9]	K. Yang, J. Wang, Z. Zhao, Z. Zhou, M. Liu, J. Zhang, Z. He, F. Zhang, ACS Appl. Mater. Interfaces 2021, 13, 21565.

[10]	M. Jeong, S. G. Han, W. Sung, S. Kim, J. Min, M. K. Kim, W. Choi, H. Lee, D. Lee, M. Kim, K. Cho, Adv. Funct. Mater. 2023, 33, DOI 10.1002/adfm.202300695.

[11]	Y. Huang, L. Shao, Y. Wang, L. Hao, X. Luo, J. Zheng, Y. Cao, S. Li, Z. Tan, S. Li, W. Zhong, S. Dong, X. Yang, J. Benduhn, C. Liu, K. Leo, F. Huang, Advanced Materials 2025, 37, DOI 10.1002/adma.202500491.

[12]	J. Xiao, J. Wu, F. Zhu, J. Ke, Q. Liu, Y. Wang, L. Yuan, H. Tai, Y. Jiang, Adv. Funct. Mater. 2024, 34, DOI 10.1002/adfm.202404711.

[13]	S. Li, Y. Wang, L. Hao, Z. Tan, Y. Huang, W. Zhong, S. Dong, X. Yang, F. Huang, Adv. Funct. Mater. 2025, 35, DOI 10.1002/adfm.202415142.

[14]	D. Guo, D. Yang, J. Li, G. He, J. Li, J. Fu, L. Wang, D. Ma, Appl. Phys. Lett. 2023, 123, DOI 10.1063/5.0177719.

[15]	L. C. Winkler, J. Kublitski, J. Benduhn, K. Leo, Adv. Electron. Mater. 2023, 9, DOI 10.1002/aelm.202201350.

[16]	A. Sarwar, Y. Wang, L. C. Winkler, T. Zhang, J. Schröder, D. Spoltore, K. Leo, J. Benduhn, Adv. Funct. Mater. 2025, 35, DOI 10.1002/adfm.202424456.

[17]	D. Guo, D. Yang, J. Zhao, A. Vadim, D. Ma, J. Mater. Chem. C Mater. 2020, 8, 9024.

[18]	N. Li, J. Lim, J. D. Azoulay, T. N. Ng, J. Mater. Chem. C Mater. 2020, 8, 15142.